Copper Berillium Jumpers for the Barrel Modules

Building and QA

- Kapton Tape - Starting with  Jumper stock from Laird,  add 2 cm width kapton tape on inside of longer  metal fold  along the whole eight inch length ensuring that the tape goes from the bend to the edge along the length.

- Bend Protection – Place 6 strips of 1” X 8.5” paper (.027”)  along the length on the inside of the jumper stock.

- Cut Strips - Cut jumper into strips .56” wide using a  paper cutter.  Leave cut paper inside fold.

- Indicate Slot Location - Mark bend side of the jumper strip with scribe to indicate final location of bent metal using plastic jig with tab referenced to one edge.

- Cut Fold Bevels - Using scissors cut long bevel from side to jumper fold  where tab mark is on both sides.  Remove paper from fold.

- Cut Paddle Ends - Cut longer jumper strip end (side with kapton) to  make rounded shovel shape for RF finger sides.  Then cut corners off shorter strip leaving a flat on inside is OK since a spatula will be used to push it in.

- Inspect cuts - Inspect and cut/break off any sharp edges or splinters on cut edges.  We have a rotary tool nearby that allows us to grind down suspect corners/breaks etc.

- Edge Sanding - Using 240 or 320 grit sand paper sand cut edges.  One at a time, push the shorter paddle laterally slightly off to each side with respect to larger paddle and slide corners across sand paper to eliminate sharp point.

- Inner Surface Sanding -  Place jumper over two back to back sheets of sand paper and slide applying slight pressure to Cu Be pads to sand sharp edges inside fold.

- Slot Width Check - Check width of material at bend using calipers:

  - Thin slots:  Must be  < .155”

  - Wide slots Must be   < .32”

A very close fit is OK.

2

3

4

5

6

10